## Slide 1: Scaffold Fabrication Strategies for Wound Healing By: Morteza Khodaei Supervisor: Dr. Mehdinavaz Spring 2025
School of metallurgy and Material science, University of Tehran

## Slide 2: Table of contents 01 03 02 04
Introduction
Methods
Conclusion & Summary
Case Studies

## Slide 3: Introduction 01

## Slide 4: Background on Wound Healing
Chronic wounds and surgical scars pose significant medical challenges
Scaffold-based strategies are promising for enhanced healing
Aims: mimic ECM, support cell activity, and control healing environment
1

## Slide 5: What Makes an Ideal Scaffold
Bio-compatibility
Drug loading capacity
High porosity
Bio-degradability
Inter-connectivity
Mechanical stability
2

## Slide 6: Methods 02

## Slide 7: Fabrication Methods
Freeze-drying
Simple
Cost-effective
High porosity
Poor control
Drug loaded hydrogel
Electrospinning
3D Printing
Produces ECM-Like nanofiber meshes
Good for surface interactions
Limited mechanical strength
High reproducibility in 2D/3D mats
Layer-by-layer precision
Multi-material and cell incorporation
Custom design for complex wound shapes
High cost
high potential
3

## Slide 8: Case Studies 03

## Slide 9: Case Studie 1: 3D printed Aloe barbadensis loaded alginate-gelatin hydrogel
4

## Slide 10: Case Studie 1
Porous and interconnected structure facilitating cell infiltration
SEM Images of 3D-Printed ALG-GE-AVE Hydrogels
5

## Slide 11: Case Studie 1
H) Histogram of the average pore size distribution of SA-G-ALB scaffold, I) Histogram of the average strut width of SA-G scaffold, J) Histogram of the average strut width of SA-G scaffold, K) Stress-strain curve of both SA-G and SA-G-ALB scaffolds L) Mechanical properties of both SA-G and SA-G-ALB scaffold.
6

## Slide 12: Case Studie 2: Degree of sulfation of freeze-dried calcium alginate sulfate scaffolds
7

## Slide 13: Case Studie 2
SEM images of the surface and cross-section of neat alginate and its sulfated derivatives
11

## Slide 14: Case Studie 2
Histological analysis of H&E (epidermal layer), MT (collagen layer, green), and TB (inflammatory cells, black) staining
12
(b) histological analysis of H&E staining of samples to reveal the formation of epidermal layer, MT staining to show the collagenous layer (green) and TB staining to indicate the presence of inflammatory cells in the wound (black marker). (Scale bars = 100 μm, and n = 4 for each group per time point).

## Slide 15: Case Studie 2
Macroscopic images of wound closure across different treatment groups on day 20
Wound Closure (%) | Group
50% | Ctrl
60% | Alg
80% | Alg-s 0.2
90% | Alg-s 0.5
13

## Slide 16: Case Studie 3: Bioactive Hydrogel Based on Collagen
10

## Slide 17: Case Studie 3
8

## Slide 18: Case Studie 3
Microscopic images of C6 (a,b) and F6 (c,d) samples before (a,c) and after (b,d) incubationin SBF solution
9

## Slide 19: Conclusion & Summary 04

## Slide 20: Conclusion & Summary
Case Study | Scaffold Type | Fabrication method | Outcome
Alginate Sulfate (2024) | Freeze-dried porous scaffold | Freeze-drying | Enhanced healing, ↓ inflammation (↓TGF-β)
Aloe-Loaded Alg-Gel (2025) | 3D printed biohydrogel | 3D Bioprinting | Accelerated closure, ↓ scar formation
Collagen/HA + Placenta (2025) | ECM-mimetic hydrogel | Freeze-drying | Improved hydration, re-epithelialization
14

## Slide 21
Thanks